	
Foam/Film Underlayment for Laminate Floor Installation
AstroBarrier can be used for any application of a l
 

A patented all-in-one laminate flooring underlayment
aminate floor that requires a film and foam underlayment, including hydronically heated systems. AstroBarrier's unique construction reduces your floor preparation time by 50%! 
Just follow these simple instructions and you are well on your way to having a beautiful laminate floor.
[image: image1.jpg]



[image: image2.png]



Unroll AstroBarrier onto concrete floor. It is generally easier to place the film side down. However, the foam side can be placed down if preferred.

[image: image3.png]



Make sure when unrolling subsequent rolls that the film-edge overlaps the adjacent roll edge completely. (If the film overlap is less than 4", taping is required to obtain a uniform vapor-barrier.) 

[image: image4.png]



Allow for a 3" - 4" overlap of AstroBarrier at the perimeter of the room. Let the excess curl up on the wall edge.

[image: image5.png]



Install laminate floor as directed by the manufacturer over AstroBarrier.

 

AstroBarrier, AstroBarrier II, and AstroFoam
Technical Data Sheet
Physical Property

Nominal Density

Compression Strength

Impact Sound Trans.

Sound Trans. Loss

Vapor Trans. Rate

Vapor Trans. Rate

Vapor Barrier

Working Temp.

Linear Shrinkage

Chemical Resistance

Tensile Strength

Elongation

Tear Srength

Water Absorption

Gauge

Thermal Resistance

Units

PCF

PSI

IIC

STC

Gxsq/m/day

Gxsq/in/day

3 mils

F

%

N/A

PSI

%

Lbf/m

%

Inch

R-Value

Typical/Properties

1.985-2.225

2.0-3.5@ 30%

47

50

26.1 (AstroFoam)

4.2 (AstroBarrier & II)

PE Film

-65 to + 165

<5&

Excellent

70-86

76-80

6.6-8.7

<01

.075 (5/64")

0.30R

Test Method

ASTM-D-3575

ASTM-D-3575

ASTM-E-492-90

ASTM-E-90-90

DIN 52615

DIN52615

 

ASTM-D-3573

ASTM-D-3575

ASTM-D-3575

ASTM-D-412

ASTM-D-412

ASTM-D-624

ASTM-D-3575

 

ASTM-C-518

All-In-One Film/Foam Laminate Floor Underlayment

 




[image: image6.png]



