
	Reflective Rigid Foam Board Insulation
Designed For Metal & Post-Frame Buildings

	 
	 
	 

	Superior Performance - Lightweight
• Provides a seamless layer of protection that reduces
   unwanted air flow
• Built tough to resist puncture and corrosion
• White surface brightens interior and establishes
   safer environment
• 4' x 50' bundle weighs just 16 pounds
• Will not compress between purlins & roof deck
  

Prevents Costly Moisture Damage
• Waterproof - will not absorb water
• Surface captures and channels rainwater and
   condensation to roof overhang areas
• Engineered to keep stored material, equipment,
   and livestock dry

Easy Installation - Saves Time & Money
• Attaches over or under roof purlins
• Attaches outside sidewall girts
• 4' x 50' continuous bundle covers 200 sq. ft.
• Unique fanfold makes placement a snap
    -Simply unfold across frame
    -Attach with staples or screws
    -Trim with utility knife
	[image: image1.jpg]




	USE IN SIDEWALL AND ROOFING INSTALLATIONS FOR:
ANIMAL CONFINEMENT       PRODUCT STORAGE
MACHINE/EQUIPMENT STORAGE      DAIRY BARNS
POULTRY FARMS      DRYING & CURING AREAS
OTHER APPLICATIONS
	 

	  
Specifications:
	 
	 

	Thickness:
Weight:
Flame Spread Index: ASTM E 84 / UL 723
Smoke Developed Index: ASTM E 84 / UL 723
Fire Rating: NFPA 255 / UBC 42-1
Reflectivity/Emissivity: ASTM C 1371
R-Value: ASTM C 518
Water Vapor Transmission: ASTM E 96
Max. Recommended Use Temperature:
	1/4" Nominal
80 pounds per 1000 sq. ft.
5
25
Class A / Class 1
94% / 6%
6.5 (Down), 3.8 (Horiz.), 3.6 (Up)
0.6
165°F
	 


 

 

