 
	Safe and Energy Efficient
Made from 100% Polyester Thermally bonded Hiloft Nonwoven fiber, laminated to 99% Pure Reinforced Aluminum foil. 

An easy to clean surface that maintains duct temperature between cycles; adding occupant comfort and minimizing run time. Enhances thermal performance and minimizes friction loss. Improves the performance of in-duct UV sanitizers. 
Superior Acoustical Performance
Greatly reduces operating noise transfer.
Noise Reduction Coefficient Rating 0.75
	[image: image1.jpg]





	

	Specifications:
Reflectivity:
ASTM C1371
97%
Emissivity:
ASTM C1371
3%
Hot Surface:
ASTM C411
Zero Warpage
Flame Spread:
ASTM E84
15
Smoked Developed:
ASTM E84
10
R-Value:
ASTM C518
4.2
Permeance:
ASTM G21, G22
Zero Growth
UV Reflection:
D & S Solar Reflectometer
>75%
[image: image2.jpg]




[image: image3.jpg]



State of California Bureau of Home Furnishings & Thermal Insulation Registry No. CA-T398 (IN). City of LA Department of Buildings & Safety RR-8403.



Astro-Safe is completely safe for installers, building owners and occupants. Astro-Safe's acoustical and thermal performance is the best available. The smooth foil surface assures minimum air friction loss and acts as an additional insulator preventing heat loss or gain between blower cycles. The tough foil surface allows ducts to be cleaned with standard rotating brush systems. Available in ½" & 1" thickness. Standard roll size: 4' x 50', custom cuts are available.





